Detailed description of drawing

Figure 1

The schematic diagram of the Regulated Adjustable Power Supply Generator and its methodology employed to produce colloidal silver nanoparticles, as presented in Figure 1.

Detailed description of drawing

Figure 2

The silver atoms generated at the cathode experiencing nucleation and subsequent growth, which ultimately leads to the formation of the colloidal silver nanoparticles, as illustrated in figure 2.

Detailed description of drawing

Figure 3

Scanning Electron Microscopy Results for Silver Nanoparticle

Detailed description of drawing

Figure 4

Transmission Electron Microscopy of silver nanoparticle

Detailed description of drawing

| Summary |  | Percentiles |  |
| --- | --- | --- | --- |
| Data | Value | %Title | Size (nm) |
| MV (nm) | 2.780 | 10.00 | 4.01 |
| MN (nm) | 2.190 | 20.00 | 3.36 |
| MA (NM) | 2.520 | 30.00 | 3.01 |
| CS | 2381 | 40.00 | 2.743 |
| SD | 0.820 | 50.00 | 2.532 |
| PDI | 50.57 | 60.00 | 2.354 |
| Mz | 2.680 | 70.00 | 2.179 |
| σι | 0.862 | 80.00 | 2.006 |
| Ski | 358.6 | 90.00 | 1.822 |
| Kg | 1146 | 95.00 | 1.705 |

Figure 5

Particle size distribution results of colloidal silver nanoparticles solution

| Measured Data |  |
| --- | --- |
| Zeta Potential | 32.8 mv |
| Polarity | Negative |
| Mobility | 2.5 µ/s/V/sm |
| Conductivity | 139 µS/cm |
| Field Strength | 9.9 kV/m |
| SOP |  |
| Zeta Run Time | 30 sec |

Detailed description of drawing

Figure 6

Zeta potential results of colloidal silver nanoparticle solution

Detailed description of drawing

Figure 7

UV-VIS (Ultraviolet-Visible) spectroscopy results for of silver nanoparticles colloidal solution.